## Slide 1
Foam Defect Catalog
Hyundai Tucson TLe
Hyundai i30
PDe

## Slide 2: TLe
Foam Defect Catalog
Project
Front
Rear

## Slide 3: PDe
Front
Rear
Foam Defect Catalog
Project

## Slide 4: TLe Front
Foam Defect Catalog
Project
TLe
A
B
C
D
A
B
B
B
C
D
D
D
Equipment

## Slide 5: TLe Front→ ZONE A
Repair
Foam Defect Catalog
Project
TLe
A
TLe Front
1
2
3
4
A-1
Defect reason | RP-02 Missing material
Size H/W/D [mm] | 15/25/15
Manifestation | Hole when cover is used
NG
OK
NG

## Slide 6: TLe Front→ ZONE A
Repair
Foam Defect Catalog
Project
TLe
TLe Front
A-2
Defect reason | RP-02 Missing material
Size H/W/D [mm] | 10/20/20
Manifestation | Hole when cover is used
NG
OK
A
1
2
3
4

## Slide 7: TLe Front→ ZONE A
Repair
Foam Defect Catalog
Project
TLe
TLe Front
A-3
Defect reason | RP-02 Missing material
Size H/W/D [mm] | 15/15/20
Manifestation | Hole when cover is used
NG
NG
OK
A
1
2
3
4

## Slide 8: TLe Front→ ZONE A
Repair
Foam Defect Catalog
Project
TLe
TLe Front
A-4
Defect reason | RP-02 Missing material
Size H/W/D [mm] | 20/30/15
Manifestation | Hole when cover is used
NG
OK
A
1
2
3
4

## Slide 9: TLe Front → ZONE B
Repair
Foam Defect Catalog
Project
TLe
TLe Front
B
1
2
Defect reason | RP-02 Missing foam
Size H/W/D [mm] | 40/15/15
Manifestation | Bulge when cover is used
B-1
NG
NG
OK

## Slide 10: TLe Front → ZONE B
Repair
Foam Defect Catalog
Project
TLe
TLe Front
Defect reason | RP-02 Missing foam
Size H/W/D [mm] | 30/30/15
Manifestation | Bulge when cover is used
B-2
NG
NG
OK
B
1
2

## Slide 11: TLe Front → ZONE C
Foam Defect Catalog
Project
TLe
TLe Front
C
1
2
C-1
Defect reason | RP-02 Missing material
Size H/W/D [mm] | 15/15/20
Manifestation | Hole when cover is used
Repair
NG
OK

## Slide 12: TLe Front → ZONE C
Repair
Foam Defect Catalog
Project
TLe
TLe Front
C-2
Defect reason | RP-02 Missing material
Size H/W/D [mm] | 15/15/20
Manifestation | Hole when cover is used
NG
NG
OK
C
1
2

## Slide 13: TLe Front → ZONE D
Foam Defect Catalog
Project
TLe
TLe Front
D
1
2
3
4
Repair
Inner Look
NG
NG
Outer Look
Defect Foam
Defect Seat
Defect reason | RP-01 Hole under suface
Size H/W/D [mm] | 20/15/15
Manifestation | Surface cover deformation
D-1
OK
5

## Slide 14: TLe Front → ZONE D
Foam Defect Catalog
Project
TLe
TLe Front
Repair
Defect reason | RP-06 Deformation
Size H/W/D [mm] | 25/100/10
Manifestation | Wrincled and deformated cover
D-2
NG
NG
OK
D
1
2
3
4
5

## Slide 15: TLe Front → ZONE D
Repair
Foam Defect Catalog
Project
TLe
TLe Front
Defect reason | RP-02 Missing material
Size H/W/D [mm] | 60/25/45
Manifestation | Hole and wrinkles when cover is used
NG
NG
OK
D-3
D
1
2
3
4
5

## Slide 16: TLe Front → ZONE D
Repair
Foam Defect Catalog
Project
TLe
TLe front
Defect reason | RP-0X Wrong repair
Size H/W/D [mm] | 20/15/15
Manifestation | Bulge when cover is used
Description- Technically, rework has been done correctly- foam is warm and soft and after cool down gets harder so BULGE appears
NG
NG
OK
D-4
D
1
2
3
4
5

## Slide 17: TLe Front → ZONE D
Repair
Foam Defect Catalog
Project
TLe
TLe Front
Defect reason | RP-04 Overflow
Size H/W/D [mm] | 20/15/15
Manifestation | Hard overflowed foam
D-5
NG
NG
OK
D
1
2
3
4
5

## Slide 18: TLe Front Equipment
Foam Defect Catalog
Project
TLe
TLe Front
SAB
SBR
Heater
Cush
Heater Back

## Slide 19: TLe Front Equipment
Red zone (SAB) HAS TO be with NO defect
Max possible repair 15x10 mm
Deffect over 15x10 mm=SCRAP
Torn foam SAB area NG (Img 1;3)
Foam Defect Catalog
Project
TLe Front
SAB-1
SAB
1
Official OK
Official OK
NG
NG
NG
Hole through
Equipment
3
2
1
NG
4